PCD 784:2026

ICS: 59.080.30

DRAFT ZANZIBAR NATIONAL STANDARD

Textiles – Scarf — Specification

ZANZIBAR BUREAU OF STANDARDS

©ZBS 2026 - All rights reserved   				                                          First edition

Foreword

## This Draft Zanzibar National Standard has been prepared by Textiles and Leather Standards Technical Committee (TCC3). In accordance with the Zanzibar Bureau of Standard general procedures, this draft standard is here by presented to the public in order to receive any technical comment concerns.

## The ZBS was established under the Standard Act No. 1 of 2011.

## In the preparation of this Standard, the reference was made to the following sources:

## SANS 1261-2:2008, Performance requirements for retail textiles - Part 2: Piece-goods for women’s and girls’ wear

## Technical Committee Representatives

## This Draft Zanzibar National Standard was prepared by Textiles and Leather Standards Technical Committee (TCC3) which consists of representatives from the following organizations:

## Chief Government Chemist Laboratory Agency (CGCLA)

## College of Engineering and Technology (CoET)

## Special Department Industrial Unit (SPEDIU)

## Zanzibar National Chamber of Commerce (ZNCC)

## Zanzibar Fisheries and Marine Resources Research Institute (ZAFIRI)

## Zanzibar Bureau of Standards (ZBS) – Secretariat

## Zanzibar Bureau of Standards (ZBS)

## PO Box 1136

## Zanzibar

## Tel:  +255 24 2232225

## Fax: +255 24 2232225

## E-mail: info@zbs.go.tz

## Web: www.zbs.go.tz

Textiles – Scarf — Specification

# Scope

This Draft Zanzibar National Standard specifies the requirements, sampling and test methods for woven and knitted scarves and fabrics intended for their manufacture.

It does not specify design and finishing.

This standard is not applicable to abaya scarves.

# Normative references

The following referenced documents are indispensable for the application of this draft Zanzibar National Standard. For dated references, only the edition cited applies. For undated references, the latest edition of the referenced document (including any amendments) applies:

ISO 105-B01, Textiles — Tests for colour fastness — Part B01: Colour fastness to light: Daylight.

ISO 105-B02, Textiles — Tests for colour fastness — Part B02: Colour fastness to artificial light: Xenon arc fading lamp test.

ISO 105-C10, Textiles — Tests for colour fastness — Part C10: Colour fastness to washing with soap or soap and soda.

ISO 105-D01, Textiles — Tests for colour fastness — Part D01: Colour fastness to dry cleaning.

ISO 105-E04, Textiles — Tests for colour fastness — Part E04: Colour fastness to perspiration.

ISO 105-X11, Textiles — Tests for colour fastness - Part X11: Colour fastness to hot pressing.

ISO 105-X12, Textiles —Tests for colour fastness — Part X12: Colour fastness to rubbing.

ISO 1833, Textiles — Quantitative chemical analysis.

ISO 2859-1: Sampling procedures for inspection by attributes. Part 1: Sampling schemes indexed by acceptance quality limit (AQL) for lot-by-lot inspection.

ISO 3071, Textiles — Determination of pH of the aqueous extract.

ISO 3801, Textiles — Woven fabrics — Determination of mass per unit length and mass per unit area.

ISO 6330, Textiles — Domestic washing and drying procedures for textile testing.

ISO 12945-2, Textiles — Determination of fabric propensity to surface pilling, fuzzing or matting — Part 2: Modified Martindale method.

ISO 8559‑2, Size designation of clothes — Part 2: Primary and secondary dimension indicators.

ISO 13934-1, Textiles — Tensile properties of fabrics — Part 1: Determination of maximum force and elongation at maximum force using the strip method.

ISO 13935-1, Textiles — Seam tensile properties of fabrics and made-up textile articles — Part 1: Determination of maximum force to seam rupture using the strip method.

ISO 13936-1, Textiles — Determination of the slippage resistance of yarns at a seam in woven fabrics

Part 1: Fixed seam opening method.

ISO 13937-4: Textiles — Tear properties of fabrics. Part 4: Determination of tear force of tongue-shaped test specimens (Double tear test).

ISO 13938, Textiles — Bursting properties of fabrics

ISO 14362-3, Textiles — Methods for determination of certain aromatic amines derived from azo colorants. Part 3: Detection of the use of certain azo colorants, which may release 4-aminoazobenzene.

ISO 22198, Textiles — Fabrics — Determination of width and length

# Terms and definitions

For the purposes of this draft Zanzibar National Standard, the following term and definition shall apply;

scarf

textile article made from woven or knitted fabric worn around the head, neck or shoulders

# Requirements

## General requirements

### Fiber composition and proportion

# The fiber composition and proportion of the scarf and fabrics intended for their manufacture shall be as declared on the label, when tested in accordance with the relevant part(s) of ISO 1833.

# Where the scarf and fabrics intended for their manufacture is made from blend of two or more fibers, the fiber composition and proportion shall be as declared on the label, subject to a tolerance of ±5 %, when tested in accordance with the relevant part(s) of ISO 1833.

### Defects

#### Scarf and fabrics intended for their manufacture shall be free from manufacturing and tailoring defects including but not limited to:

# holes;

# cuts;

# tears;

# spots;

# stains;

# stitching defects such as skipped stitches and uneven stitch length;

# seaming defects such as seam slippage, seam puckering and seam grin;

# loose ends;

# uneven dyeing;

#### Scarf and fabrics intended for their manufacture shall also be free from any other defect which may significantly mar their appearance or affect their performance.

### Workmanship and finishing

#### Seam finishing

# The ends of all seams and stitching and all breaks in the thread shall be securely stitched. Stitches shall present a regular even appearance without fabric puckering.

# All raw edges shall be suitably finished.

#### Hems

# Hems shall be securely finished in such a manner as to avoid fraying and opening.

## Specific requirements

### Fabric construction requirements

### The construction requirements of fabrics intended for or used in the manufacture of scarf shall comply with the requirements given in Table 1 when tested in accordance with the test methods specified therein.

### Table 1: Construction requirements of the scarf or fabrics used in their manufacture

| S/NO | Characteristics | Requirements | Test methods |
| --- | --- | --- | --- |
|  | Mass per unit area, g/m2, min. | 55 | ISO 3801 |
|  | Breaking strength a (both warp and weft direction), N, min. | 100 | ISO 13934-1 |
|  | Tear strength a (tongue tear) in warp and weft direction), N, min. | 5 | ISO 13937-4 |
|  | Slippage resistance of yarns at a seam a, mm, max. | 4 | ISO 13936-1 |
|  | Seam strength a, N, min. | 80 | ISO 13935-1 |
|  | Piling resistance grade at 2000 rubs, min. | 4 | ISO 12945-2 |
|  | Dimensional change after five washings, %, max. | ±3a ±5b | ISO 6330 |
|  | Bursting strength b, kPa, min. | 160 | ISO 13938 |
| a Applicable to woven scarf. b Applicable to knitted scarf. |  |  |  |

## pH requirement

When tested in accordance with ISO 3071, the pH of scarf or fabrics used in their manufacture shall be 6.0 – 8.5.

## Number of Stitches

If sewed, the number of stitches shall not be less than 2 stitches per centimeter.

## Colour fastness requirements

The colour of the dyed scarf or fabrics used in their manufacture shall be fast to agencies in accordance with the requirements specified in Table 2, when tested in accordance with test methods specified therein.

Table 2: Colour fastness requirements of the dyed scarf or fabrics used in their manufacture

| S/NO | Colour fastness to: |  | Requirements | Test methods |
| --- | --- | --- | --- | --- |
|  | Light, min. |  | 4 | ISO 105-B01 and ISO 105-B02 |
|  | Rubbing, min. | Dry | 4 | ISO 105-X12 |
|  |  | Wet | 3 - 4 |  |
|  | Washing, min. | Change in colour | 4 | ISO 105-C10 |
|  |  | Staining |  |  |
|  | Hot pressing, min | Dry | 4 | ISO 105-X11 |
|  |  | Wet |  |  |
|  | Dry cleaning, min | Change in colour | 4 | ISO 105-D01 |
|  |  | Staining |  |  |
|  | Perspiration Acid solution & Alkaline, min | Change in colour | 4 | ISO 105-E04 |
|  |  | Staining | 3 - 4 |  |

## Dye properties and related requirements

Dye properties and related requirements for the dyed scarf or fabrics used in their manufacture shall be non-carcinogenic non-allergenic and free from azo dyestuffs/pigment when tested in accordance with ISO 14362.

## Size

When tested in accordance with ISO 8559‑2, the size of scarf shall be as declared on the label with tolerance of - 2%.

## Dimensions of the fabric

### The fabrics roll intended for the manufacture of scarf shall have a length of not be less than 95% and width of not less than 98%, as indicated on the label when tested in accordance with ISO 22198.

# Packaging and labelling

## Packaging

## The following shall be considered on packing:

## Scarf or the fabric roll intended for their manufacture shall be packed in suitable waterproof materials to avoid contamination during transportation and storage; and

## Each scarf shall be packed in a separate bag or a separate sealed box or both.

## Labelling

### Unit package

Each piece of scarf or the fabric roll intended for their manufacture shall be legibly and indelibly labelled with the following information:

a) name of the product;

b) fibre composition, expressed as a percentage by mass;

c) size of the scarf or dimensions of the fabric roll (length × width);

e) care instructions, using symbols or words;

f) name and physical address of the manufacturer, importer, or distributor;

g) country of origin; and

h) batch number, lot number, or production date;

### Bulk package

Bulk packages containing scarf or fabric intended for their manufacture shall be legibly and indelibly labelled with the following information:

a) name of the product;

b) fibre composition, expressed as a percentage by mass;

c) name and physical address of the manufacturer, importer or distributor;

d) country of origin;

e) batch number, lot number or production date;

f) net quantity (number of unit packages or length of fabric);

### The language on the label shall be ‘Swahili’ and/or English. Additional language may be used depending on the designated market.

# Sampling

Sampling shall be done in accordance with ISO 2859-1